B90: MAINTENANCE, ALTERATION, AND QUALIFICATION OF TANK CAR STUB SILLS

| Car Mark/Number | PAWCT-B90 |  |  |
| --- | --- | --- | --- |
| Repair Level | RLS |  |  |

SPECIAL PROCESS (Welding)

| WPS Number | DLG W-No.07-1 |  |  |
| --- | --- | --- | --- |
| WPS Voltage | 24-28 V | Observed Voltage | MISSING DATA |
| Filler Metal | E71T-1 | Observed | E71T-9C H8 |

NON-DESTRUCTIVE TESTING (NDT)

| NDT Tech ID | Level | Expiration |
| --- | --- | --- |
| DLGA/NDT-47 | Level II | 2028-02-25 |

QUALITY RECORDS AND TEST RECORDS

Description of Work: Maintenance, Alteration, and Qualification of Tank Car Stub Sills

AUDITOR NOTES/WARNINGS: Observed welding parameters (actual amps/volts during demonstration) not identified. | Visual inspection final acceptance disposition not clearly identified. | Inspector signoff not clearly identified. | PITP evidence not explicitly identified. | TCID evidence not identified. | Multiple B90 welding machine IDs found in source set (DLG-MS-02 and DLG-MS-20); equipment fields set to null for manual review. | Filler classification review required: WPS/WQR specify E71T-1 while observed spool shows E71T-9C H8. | Do not use historical procedure approval signatures as current audit signoff.

SIGN-OFF: REQUIRES 2026 AUDITOR SIGNATURE