EXHIBIT B-2: B90 OBJECTIVE EVIDENCE (PAGE 1)

| Car Mark/Number | PAWCT-B90 |
| --- | --- |
| Material Spec | ASTM A572 Grade 50 |

WELDING DATA & EQUIPMENT (PAGE 2)

| Parameter | Requirement | Observed |
| --- | --- | --- |
| WPS ID | DLG W-No.07-1 | MATCHED |
| Voltage | 24-28 V | MISSING DATA |

PERSONNEL QUALIFICATIONS & NDT (PAGE 3)

| Technician Name |  |
| --- | --- |
| Certification Level | Level II |
| Expiration Date | 2028-02-25 |
| Method | VT |

QA RECORDS & FINAL DISPOSITION (PAGE 4)

AUDIT WARNINGS: Observed welding parameters (actual amps/volts during demonstration) not identified. | Visual inspection final acceptance disposition not clearly identified. | Inspector signoff not clearly identified. | PITP evidence not explicitly identified. | TCID evidence not identified. | Multiple B90 welding machine IDs found in source set (DLG-MS-02 and DLG-MS-20); equipment fields set to null for manual review. | Filler classification review required: WPS/WQR specify E71T-1 while observed spool shows E71T-9C H8. | Do not use historical procedure approval signatures as current audit signoff.

FINAL AUDITOR SIGN-OFF: ________________________ DATE: __________