B89: MAINTENANCE, MODIFICATION, AND QUALIFICATION OF SAFETY SYSTEMS

# Documentation used to perform demonstration of an insulation repair and repair level Jacket (RLJ) using a test plate.

| Car Owner’s Permission |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tank Car Owner (TCO) Name |  |  | Date Permission Received from TCO |  | Written Instructions from TCO |  |  |  |  |  |
| UTLX |  |  | 1/13/2021 |  | Choose an item.Facility received written instructions furnished by the OWNER. |  |  |  |  |  |
| DESIGN CONTROL |  |  |  |  |  |  |  |  |  |  |
| Car Mark and Number | Tank Car Design Spec/Stencil Spec |  |  |  |  | Safety System Type |  |  | AAR Form 4-2 (AAR No.) |  |
| UTLX 213220 | DOT111A100W1/DOT117R100W |  |  |  |  | Insulation/Jacket |  |  | M177033 |  |
| 4-2 Drawing Type |  |  | Drawing Number |  |  |  | Revision |  |  |  |
| General Arrangement |  |  | 512041-03F |  |  |  | G |  |  |  |
| MATERIALS |  |  |  |  |  |  |  |  |  |  |
| Description of Material(s) Used to Demonstrate Maintenance, Modification, and Qualification of Safety System |  |  |  |  |  |  | Material Specification |  |  | Material Thickness |
| Insulation |  |  |  |  |  |  | Fiberglass |  |  | 1/2" |
| Jacket Material |  |  |  |  |  |  | A1011 |  |  | 11 Gauge |
| TEST FIXTURE |  |  |  |  |  |  |  |  |  |  |
| Observed Size of Patch Plate |  |  |  | Observed Contour of Test Plate |  |  |  |  |  |  |
| 12" x 12" |  |  |  | Typical |  |  |  |  |  |  |
| Observed Test Plate Width |  | Observed Test Plate Height |  | Observed Fillet Weld Size |  |  |  | Observed Weld Length |  |  |
| 24" |  | 24" |  | 3/8" |  |  |  | 48" |  |  |
| Protective Coating Type and Date Observed |  |  |  | Black Paint- 6/10/2025 |  |  |  |  |  |  |
| Additional Auditor Objective Evidence/Comments/Notes: |  |  |  |  |  |  |  |  |  |  |
| Car file preparation, including all inspection and test records, and compliance with TCID. |  |  |  |  |  |  |  |  |  |  |

In lieu of demonstrating repair level RLJ on a tank car, a facility is permitted to use a test weldment / fixture, which is representative of an approved design including the insulation/thermal protection system. At a minimum, the test weldment / fixture.

| PERSONNEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Personnel ID |  |  |  |  |  |  |  | Function Performed |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date Received Function Specific Training |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| M. Marquez |  |  |  |  |  |  |  | Insulation Inspection |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 6/10/2025 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PROCEDURES |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PITP Document Name |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | PITP ID |  |  |  |  |  |  |  |  |  |  | Approved By |  |  |  |  |  |  |  |  |  | Date Approved |  |  |  |  |  |  |  |  |  | Rev |  |  |
| Production, Inspection, and Test |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | QP 2.5-03 |  |  |  |  |  |  |  |  |  |  | C. Gamblin |  |  |  |  |  |  |  |  |  | 6/22/2023 |  |  |  |  |  |  |  |  |  | Orig. |  |  |
| Procedures Traceable to the PITP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Procedure ID |  |  |  |  |  |  |  |  |  |  |  | Approved By |  |  |  |  |  |  |  |  |  |  | Date Approved |  |  |  |  |  |  | Rev. |
| Insulation Inspection/Qualification Procedure |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | RES041 |  |  |  |  |  |  |  |  |  |  |  | J. Riggs |  |  |  |  |  |  |  |  |  |  | 5/24/2021 |  |  |  |  |  |  | G |
| Additional Procedures Traceable to the PITP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Procedure ID |  |  |  |  |  |  |  |  |  |  | Approved By |  |  |  |  |  |  |  |  |  |  | Date Approved |  |  |  |  |  |  |  |  | Rev |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | RES162 |  |  |  |  |  |  |  |  |  |  | J. Riggs |  |  |  |  |  |  |  |  |  |  | 7/22/2024 |  |  |  |  |  |  |  |  | F |
| Record/Form Identified by the Procedure |  |  |  |  |  |  | Record/Form ID |  |  |  |  |  |  |  | Approved By |  |  |  |  |  |  |  | Date Approved |  |  |  |  |  |  |  |  | Rev. |  |  |  |  |  |  | Result (including accepted or rejected) |  |  |  |  |  |  |  |  |  |  |
| Work Order |  |  |  |  |  |  | Work Order |  |  |  |  |  |  |  | J. Riggs |  |  |  |  |  |  |  | 7/22/2024 |  |  |  |  |  |  |  |  | 7/22/2024 |  |  |  |  |  |  | Accepted/OK |  |  |  |  |  |  |  |  |  |  |
| SPECIAL PROCESSES (Welding) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Welder / Operator ID | Stamp or ID Assigned |  |  |  |  |  |  |  | Position(s) Qualified |  |  |  |  |  |  |  |  |  |  | Welder WPQR Completion Date |  |  |  |  |  |  |  | Visual Acuity Date |  |  |  |  |  |  |  |  |  | Visual Acuity Expires Date |  |  |  |  |  |  |  | Continuity Log Date |  |  |  |
| M. Marquez | MM |  |  |  |  |  |  |  | 1-4F |  |  |  |  |  |  |  |  |  |  | 9/30/2019 |  |  |  |  |  |  |  | 3/14/2025 |  |  |  |  |  |  |  |  |  | 3/14/2026 |  |  |  |  |  |  |  | 1/31/2025 |  |  |  |
| WPS Traceable to the PITP |  |  | Date WPS Approved |  |  |  |  |  |  |  |  |  | WPS Rev. |  |  |  |  |  |  |  |  | PQR supporting the WPS |  |  |  |  |  |  |  |  |  |  |  |  |  | PQR Date Completed |  |  |  |  |  |  |  |  |  |  |  | Rev |  |
| QPS 2.15.6.3 |  |  | 6/17/2024 |  |  |  |  |  |  |  |  |  | D |  |  |  |  |  |  |  |  | D15.1 Prequalified |  |  |  |  |  |  |  |  |  |  |  |  |  | NA |  |  |  |  |  |  |  |  |  |  |  | NA |  |
| Welding Process |  |  |  | WPS Joint Design |  |  |  |  |  |  |  |  |  |  |  |  | Observed Joint Design |  |  |  |  |  |  |  |  | WPS Thickness Range |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Observed Thickness |  |  |  |  |  |  |
| SMAW |  |  |  | Fillet |  |  |  |  |  |  |  |  |  |  |  |  | Fillet |  |  |  |  |  |  |  |  | 11 Gauge - 1" |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 11 Gauge |  |  |  |  |  |  |
| WPS Voltage |  | Observed Voltage |  |  |  |  |  |  |  |  |  | WPS Amperage |  |  |  |  |  |  |  |  |  | Observed Amperage |  |  |  |  |  |  |  |  |  |  |  |  | WPS Wire Feed Rate |  |  |  |  |  |  |  |  | Observed Wire Feed Rate |  |  |  |  |  |
|  |  | NA |  |  |  |  |  |  |  |  |  | 72-100 |  |  |  |  |  |  |  |  |  | 85 |  |  |  |  |  |  |  |  |  |  |  |  | Manual |  |  |  |  |  |  |  |  | Manual |  |  |  |  |  |
| Material 1: Jacket Plate Material Type/Spec & Thickness |  |  |  |  | Material 2: Jacket Patch Material Type/Spec & Thickness |  |  |  |  |  |  |  |  | WPS Electrode/Wire Material Type/Spec |  |  |  |  |  |  |  |  |  | Observed Electrode/Wire Material Type/Spec |  |  |  |  |  |  |  |  |  | WPS Electrode/Wire Diameter |  |  |  |  |  |  |  |  |  |  | Observed Electrode/Wire Diameter |  |  |  |  |
| A1011/11 Gauge |  |  |  |  | A1011/11 Gauge |  |  |  |  |  |  |  |  | 6010/6011/A5.1 |  |  |  |  |  |  |  |  |  | 6010/A5.1 |  |  |  |  |  |  |  |  |  | 1/8" |  |  |  |  |  |  |  |  |  |  | 1/8" |  |  |  |  |
| WPS Preheat Temp. |  |  |  |  |  | Observed Preheat Temp. |  |  |  |  |  |  |  |  |  |  |  |  |  | WPS Interpass Temperature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Observed Interpass Temperature |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 50°F |  |  |  |  |  | 101ºF |  |  |  |  |  |  |  |  |  |  |  |  |  | NA |  |  |  |  |  |  |  |  |  |  |  |  |  |  | NA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| EQUIPMENT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Measure and Test Equipment |  |  |  |  |  |  |  |  |  |  | ID |  |  |  |  |  |  |  |  |  |  |  |  |  | Calibration Date or In-Service Date |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Calibration Due |  |  |  |  |  |  |  |  |
| Welding Machine |  |  |  |  |  |  |  |  |  |  | U1141106957 |  |  |  |  |  |  |  |  |  |  |  |  |  | 9/19/2024 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 9/19/2025 |  |  |  |  |  |  |  |  |
| Wire Feeder |  |  |  |  |  |  |  |  |  |  | NA |  |  |  |  |  |  |  |  |  |  |  |  |  | NA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | NA |  |  |  |  |  |  |  |  |
| Thermometer |  |  |  |  |  |  |  |  |  |  | 152-17 |  |  |  |  |  |  |  |  |  |  |  |  |  | 10/10/2024 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 10/10/2025 |  |  |  |  |  |  |  |  |
| Measure and Test Equipment |  |  |  |  |  |  |  |  |  | ID |  |  |  |  |  |  |  |  |  |  | Function Performed |  |  |  |  |  |  |  |  |  |  |  | Calibration Date or In-Service Date |  |  |  |  |  |  |  |  |  |  | Calibration Due |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  | 152FW3 |  |  |  |  |  |  |  |  |  |  | Weld Gauge |  |  |  |  |  |  |  |  |  |  |  | 11/27/2023 |  |  |  |  |  |  |  |  |  |  | 11/27/2026 |  |  |  |  |  |
| Additional Auditor Objective Evidence/Comments/Notes: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Car file preparation, including all inspection and test records, and compliance with TCID. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

# At a minimum Utilizing AWS D15.1 Designee, perform a weld inspection utilizing AWS D15.1 acceptance criteria as required by Appendix B 3.6.9.6.2.5.3. In lieu of AWS D15.1 inspection ASNT VT can be used.

| AWS/D15.1 Inspection Cirteria | Choose an item. |
| --- | --- |

# If Applicable, Utilizing AWS D15.1 Designee, perform a weld inspection utilizing AWS D15.1 acceptance criteria as required by Appendix B 3.6.9.6.2.5.3.

# If Applicable, in lieu of utilizing AWS D15.1 inspection criteria an ASNT NDT Method can be used.

| PERSONNEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Personnel ID |  |  | Function Performed |  |  |  |  |  |  | Date Received Function Specific Training |  |  |  |  |  |
| M. Marquez |  |  | AWS D15.1 Weld Inspection |  |  |  |  |  |  | 6/10/2025 |  |  |  |  |  |
| NON-DESTRUCTIVE TESTING (NDT) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NDT Technician ID | NDT Level (I, II, III) |  |  | NDT Method(s) |  |  | Date Qualified |  | Qualification Expiration Date |  |  | Visual Acuity Date |  | Visual Acuity Due Date |  |
| M. Marquez | VT |  |  | 4/16/2023 |  |  |  |  | 4/16/2026 |  |  | 3/14/2025 |  | 3/14/2026 |  |
| NDT Procedures Traceable to the PITP |  |  |  |  | Procedure ID |  |  | NDT Level III Approver |  |  |  |  | Date Approved |  | Rev. |
|  |  |  |  |  | RES213 |  |  | J. Riggs |  |  |  |  | 10/19/2021 |  | L |
| Record/Form Identified by the Procedure |  | Record/Form ID |  |  |  | NDT Level III Approver |  | Date Approved |  |  | Rev |  | Result (including accepted or rejected) |  |  |
|  |  | RES213-1 |  |  |  | J. Riggs |  | 11/11/2024 |  |  | J |  | Accepted/OK |  |  |

| Performance Qualification Record (PQR) | Procedure ID | NDT Tech ID that Performed PQR | NDT Level III Approver | Date Approved | Rev. |
| --- | --- | --- | --- | --- | --- |
|  | QPS 2.15.6.3 | M. Marquez | J. Riggs | 6/17/2024 | D |

| NDT EQUIPMENT |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| NDT Equipment | ID | Function Performed |  | Calibration Date or In-Service Date | Calibration Due |
| Fillet Weld Gauge | 152FW3 | Weld Gauge |  | 11/27/2023 | 11/27/2026 |
| ENVIRONMENT |  |  |  |  |  |
| Location in facility where demonstration was observed |  |  | Shop |  |  |
| Additional Auditor Objective Evidence/Comments/Notes: |  |  |  |  |  |

# Car file preparation, including all inspection and test records, and compliance with TCID.

| QUALITY RECORDS AND TEST RECORDS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Procedures Traceable to the PITP |  |  |  | Procedure ID |  |  |  |  | Approved By |  | Date Approved |  |  | Rev. |
| TCID Procedure |  |  |  | RES217 |  |  |  |  | J. Perez |  | 10/4/2016 |  |  | D |
| Record/Form Identified by the Procedure |  | Record/Form ID |  |  |  | Approved By | Date Approved |  |  | Rev |  | Result (including accepted or rejected) |  |  |
| TCID Report |  | RES217-1 |  |  |  | J. Perez | 10/3/2016 |  |  | 10/3/2016 |  | Accepted/OK |  |  |
| Reference AAR Form 4-2 (AAR No.) | Car Mark and Number |  |  |  | Type of TCID Record Completed |  |  | TCID Entry Type |  |  |  |  | Date Performed |  |
| M177033 | UTLX 213220 |  |  |  | Choose an item. |  |  | Choose an item. |  |  |  |  | Welded Repairs Completed Record sent to Tank Car Owner 6/10/2025 |  |
| Description of work performed: |  |  | Insulation System Inspection and Repair |  |  |  |  |  |  |  |  |  |  |  |
| Additional Auditor Objective Evidence/Comments/Notes: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |