AAR M-1002 EXHIBIT B-2: B90 AUDIT REPORT (2026)

| Car Mark/Number | PAWCT-B90 |
| --- | --- |
| Welding Procedure (WPS) | DLG W-No.07-1 |
| Observed Filler Metal | E71T-9C H8 |
| NDT Technician ID | DLGA/NDT-47 |
| Audit Status | REQUIRES 2026 SIGN-OFF |
| Extraction Warnings | Observed welding parameters (actual amps/volts during demonstration) not identified.; Visual inspection final acceptance disposition not clearly identified.; Inspector signoff not clearly identified.; PITP evidence not explicitly identified.; TCID evidence not identified.; Multiple B90 welding machine IDs found in source set (DLG-MS-02 and DLG-MS-20); equipment fields set to null for manual review.; Filler classification review required: WPS/WQR specify E71T-1 while observed spool shows E71T-9C H8.; Do not use historical procedure approval signatures as current audit signoff. |