ASSOCIATION OF AMERICAN RAILROADS

Exhibit B-2 B90: AAR M-1002 Objective Evidence Collection Form

Activity Code: B90 (RLS) - Maintenance & Qualification of Stub Sills

DESIGN CONTROL & CAR DATA

| Car Mark and Number | PAWCT-B90 |
| --- | --- |
| Design Specification | AWS D15.1 |
| Material Specification | ASTM A572 Grade 50 |

WELDING EVIDENCE (WPS VS. OBSERVED)

| Parameter | WPS Requirement | Observed Actuals |
| --- | --- | --- |
| WPS Number | DLG W-No.07-1 | MATCHED |
| Voltage (V) | 24-28 V | MISSING - AUDIT FAIL |
| Filler Metal | E71T-1 | E71T-9C H8 |
| Welder ID | DLG FCAW WTCF W No 08 | VERIFIED |

CRITICAL AUDIT WARNINGS:

Observed welding parameters (actual amps/volts during demonstration) not identified. | Visual inspection final acceptance disposition not clearly identified. | Inspector signoff not clearly identified. | PITP evidence not explicitly identified. | TCID evidence not identified. | Multiple B90 welding machine IDs found in source set (DLG-MS-02 and DLG-MS-20); equipment fields set to null for manual review. | Filler classification review required: WPS/WQR specify E71T-1 while observed spool shows E71T-9C H8. | Do not use historical procedure approval signatures as current audit signoff.

AUDITOR SIGN-OFF: REQUIRES 2026 SIGN-OFF